HSBC Rochdale : New ATM Aperture

The HSBC Bank at 2 Yorkshire Street , Rochdale OL16 1EE is to be re-fitted with a new ATM  which will project further forward onto the pavement to facilitate easier access.
In order to accommodate this, the existing stone backing to the bezel of the machine needs to be replaced with a deeper section, pushing the new bezel some 63mm further forward. The existing stone is a Hard York Sandstone from Johnsons Wellfield Quarries, Crossland Hill, Huddersfield and we would propose using the same supplier for the new sections. 
See Photo sheet of 23.02.24. and Sketch 2023.018 attached.
Once the old ATM machine has been removed, we protect the top surface of the existing stone sill and infill and carefully ease off the stone surround - investigation shows this has been stuck onto the timber frame with silicone mastic. The sections will then be lifted off and set aside for re use.
Any fixings will be cut off with reciprocating hacksaw.
New stone will be brought to site cut to size and rubbed smooth to match the original and set aside on softening to protect the edges from damage.
The new jambs on each side will be taller and the timber cill cut away to allow these to be set down onto the existing stone sill and infill cheeks, and fixed with small stainless steel dowels, 75 x 6 dia in lime mortar, to locate them. The tops of the jambs will be fixed back to the timber window surround with stainless cramps and dowels, which will also locate the new head. Cramps to be fixed with stainless steel screws and the dowels in lime mortar.
At the base of the aperture we will cut down and re-use the original stone surround to provide small make up pieces for infilling at the sill level, and to provide a seating for the new bezel. Due to their size, these pieces will need to be glued in place with an epoxy resin, but bonded to new, not original stone. 
The joint sizes will be 4mm, all stones bedded and pointed in NHL 3.5 lime mixed at 2 parts to 5 parts crushed yellow stone dust (Naylor Myers Builders Merchants, from the Wellfield Quarry), fully filled and left proud to be sponged clean on completion.
Any loose or open joints in the adjacent stone work will be raked out using a thin bladed mason’s chisel or section of hacksaw blade and repointed with mortar as above.
The vertical and horizontal joints between stone and timber will be sealed with a one-part polysulphide mastic, over-paintable for decoration. 
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